# 5B

# RUBBED FINISH (MODIFIED)

(Effective January 1, 1997; Revised January 1, 2012)

This work shall be in accordance with Section 503 of the Standard Specifications:

Revise Article 503.15(b) to read:

b)	Rubbed Finish (Modified).  Surfaces requiring a Rubbed Finish (Modified) shall be designated on the plans or elsewhere in the special provisions.  These surfaces shall be stoned or ground with a suitable abrasive to remove fins or offsets in the concrete.  This rubbing shall be continued sufficiently to remove all roughness and projections and produce a uniform surface.

The resulting surface shall receive the following treatment.  Mix 1 part Portland cement and 1-1/2 parts of FA-10 sand with sufficient water to produce a grout having the consistency of thick paint.  Portland cement from the source of the cement used in the concrete shall be used in the grout.  Wet the surface of the concrete sufficiently to prevent absorption of water from the grout and apply the grout uniformly, completely filling air bubbles and holes.  Allow the grout to dry, then wet rub the surfaces with a No. 30 carborundum stone or an abrasive of equal quality, scour vigorously.  While the grout is still plastic, the surface shall be finished with a sponge rubber float removing all excess grout.  This finishing shall be done at the time when grout will not be pulled from holes or depressions.  Next allow the surface to dry thoroughly, then rub it vigorously with dry burlap to completely remove any dried grout.  No grout shall be left on the wall overnight.  When the surface of the concrete is not of uniform color after the above treatment, the Contractor shall be required to repeat the procedure as needed to obtain a uniform color.

The described finishing procedure must be completed within 24 hours of forms being removed.

Method of Measurement.  Rubbed Finish (Modified) will be measured for payment in place and the area computed in square feet (square meters) of surface area rubbed.

Basis of Payment.  Rubbed Finish (Modified) will be paid for at the contract unit price per square foot (square meter) for RUBBED FINISH (MODIFIED).

DESIGNER NOTE:

This special should be used on bridges in high visible areas.