# HOT-MIX ASPHALT BINDER AND SURFACE COURSE (D1)

Effective:  November 1, 2019

Revised:  January 1, 2026

Add the following to the end of Article 406.06(c) of the Standard Specifications:

“	The amount of HMA binder course placed shall be limited to that which can be surfaced during the same construction season.”

Revise the fifteenth through eighteenth paragraphs of Article 406.14 of the Standard Specifications to read:

“	The mixture used in constructing acceptable HMA test strips will be paid for at the contract unit price. Unacceptable HMA test strips shall be removed and replaced at no additional cost to the Department.”

Revise Article 1004.03(c) to read:

“(c) Gradation.  The coarse aggregate gradations shall be as listed in the following table.

| Use | Size/Application | Gradation No. |
| --- | --- | --- |
| Class A-1, A-2, & A-3 | 3/8 in. (10 mm) Seal | CA 16 or CA 20 |
| Class A-1 | 1/2 in. (13 mm) Seal | CA 15 |
| Class A-2 & A-3 | Cover Coat | CA 14 |
| HMA High ESAL | IL-19.0; Stabilized Subbase IL-19.0 | CA 11 1/ |
|  | SMA 12.5 2/ | CA 134/, CA 14, or CA 16 |
|  | SMA 9.5 2/ | CA 133/4/ or CA 163/ |
|  | IL-9.5 | CA 16, CM 134/ |
|  | IL-9.5FG | CA 16 |
| HMA Low ESAL | IL-19.0L | CA 11 1/ |
|  | IL-9.5L | CA 16 |

- CA 16 or CA 13 may be blended with the CA 11.

- The coarse aggregates used shall be capable of being combined with the fine aggregates and mineral filler to meet the approved mix design and the mix requirements noted herein.

- The specified coarse aggregate gradations may be blended.

- CA 13 shall be 100 percent passing the 1/2 in. (12.5mm) sieve.”

Revise Article 1004.03(e) of the Standard Specifications to read:

“(e) Absorption. For SMA the coarse aggregate shall also have water absorption

≤ 2.0 percent.”

Revise the “High ESAL” portion of the table in Article 1030.01 to read:

| “High ESAL | Binder Courses | IL-19.0, IL-9.5, IL-9.5FG, IL-4.75, SMA 12.5, SMA 9.5 Stabilized Subbase IL-19.0 |
| --- | --- | --- |
|  | Surface Courses | IL-9.5, IL-9.5FG, SMA 12.5, SMA 9.5” |

Revise Note 2. and add Note 6 to Article 1030.02 of the Standard Specifications to read:

“Item                                                                                  Article/Section

(g)Performance Graded Asphalt Binder (Note 6)                                  	1032

(h)	Fibers (Note 2)

Note 2. A stabilizing additive such as cellulose or mineral fiber shall be added to the SMA mixture according to Illinois Modified AASHTO M 325.  The stabilizing additive shall meet the Fiber Quality Requirements listed in Illinois Modified AASHTO M 325.  Prior to approval and use of fibers, the Contractor shall submit a notarized certification by the producer of these materials stating they meet these requirements. Reclaimed Asphalt Shingles (RAS) may be used in Stone Matrix Asphalt (SMA) mixtures designed with an SBA polymer modifier as a fiber additive if the mix design with RAS included meets AASHTO T305 requirements. The RAS shall be from a certified source that produces either Type I or Type 2. Material shall meet requirements noted herein and the actual dosage rate will be determined by the Engineer.

Note 6. The asphalt binder shall be an SBS PG 76-28 when the SMA is used on a full-depth asphalt pavement and SBS PG 76-22 when used as an overlay, except where modified herein. The asphalt binder shall be a SBS PG 76-22 for IL-4.75, except where modified herein..”

Revise table in Article 1030.05(a) of the Standard Specifications to read:

| “MIXTURE COMPOSITION (% PASSING) 1/ |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sieve Size | IL-19.0 mm |  | SMA 12.5 |  | SMA 9.5 |  | IL-9.5mm |  | IL-9.5FG |  | IL-4.75 mm |  |
|  | min | max | min | max | min | max | min | max | min | max | min | max |
| 1 1/2 in (37.5 mm) |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 in. (25 mm) |  | 100 |  |  |  |  |  |  |  |  |  |  |
| 3/4 in. (19 mm) | 90 | 100 |  | 100 |  |  |  |  |  |  |  |  |
| 1/2 in. (12.5 mm) | 75 | 89 | 80 | 100 |  | 100 |  | 100 |  | 100 |  | 100 |
| 3/8 in. (9.5 mm) |  |  |  | 65 | 90 | 100 | 90 | 100 | 90 | 100 |  | 100 |
| #4 (4.75 mm) | 40 | 60 | 20 | 30 | 36 | 50 | 34 | 69 | 60 | 756/ | 90 | 100 |
| #8 (2.36 mm) | 20 | 42 | 16 | 24 4/ | 16 | 324/ | 34 5/ | 52 2/ | 45 | 606/ | 70 | 90 |
| #16 (1.18 mm) | 15 | 30 |  |  |  |  | 10 | 32 | 25 | 40 | 50 | 65 |
| #30 (600 m) |  |  | 12 | 16 | 12 | 18 |  |  | 15 | 30 |  |  |
| #50 (300 m) | 6 | 15 |  |  |  |  | 4 | 15 | 8 | 15 | 15 | 30 |
| #100 (150 m) | 4 | 9 |  |  |  |  | 3 | 10 | 6 | 10 | 10 | 18 |
| #200 (75 m) | 3.0 | 6.0 | 7.0 | 9.0 3/ | 7.5 | 9.5 3/ | 4.0 | 6.0 | 4.0 | 6.5 | 7.0 | 9.0 3/ |
| #635 (20 m) |  |  | ≤ 3.0 |  | ≤ 3.0 |  |  |  |  |  |  |  |
| Ratio Dust/Asphalt Binder |  | 1.0 |  | 1.5 |  | 1.5 |  | 1.0 |  | 1.0 |  | 1.0 |

  - Based on percent of total aggregate weight.

  - The mixture composition shall not exceed 44 percent passing the #8 (2.36 mm) sieve for surface courses with Ndesign = 90.

  - Additional minus No. 200 (0.075 mm) material required by the mix design shall be mineral filler, unless otherwise approved by the Engineer.

  - When establishing the Adjusted Job Mix Formula (AJMF) the percent passing the #8 (2.36 mm) sieve shall not be adjusted above the percentage stated on the table.

  - When establishing the Adjusted Job Mix Formula (AJMF) the percent passing the #8 (2.36 mm) sieve shall not be adjusted below 34 percent.

  - When the mixture is used as a binder, the maximum shall be increased by 0.5 percent passing.”

Revise Article 1030.05(b) of the Standard Specifications to read:

(b) Volumetric Requirements.  The target value for the air voids of the HMA shall be 4.0 percent, for IL-4.75 and SMA mixtures it shall be 3.5 percent and for Stabilized Subbase it shall be 3.0 percent at the design number of gyrations.  The voids in the mineral aggregate (VMA) and voids filled with asphalt binder (VFA) of the HMA design shall be based on the nominal maximum size of the aggregate in the mix and shall conform to the following requirements.

|  | Voids in the Mineral Aggregate (VMA), % Minimum for Ndesign |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Mix Design | 30 | 50 | 70 | 80 | 90 |
| IL-19.0 |  | 13.5 | 13.5 |  | 13.5 |
| IL-9.5 |  | 15.0 | 15.0 |  |  |
| IL-9.5FG |  | 15.0 | 15.0 |  |  |
| IL-4.751/ |  | 18.5 |  |  |  |
| SMA-12.51/2/5/ |  |  |  | 17.03//16.04/ |  |
| SMA-9.51/2/5/ |  |  |  | 17.03//16.04/ |  |
| IL-19.0L | 13.5 |  |  |  |  |
| IL-9.5L | 15.0 |  |  |  |  |

- Maximum draindown shall be 0.3 percent according to Illinois Modified AASHTO T 305.

- The draindown shall be determined at the JMF asphalt binder content at the mixing temperature plus 30°F.

- Applies when specific gravity of coarse aggregate is ≥ 2.760.

- Applies when specific gravity of coarse aggregate is < 2.760.

- For surface course, the coarse aggregate can be crushed steel slag, crystalline crushed stone or crushed sandstone. For binder course, coarse aggregate shall be crushed stone (dolomite), crushed gravel, crystalline crushed stone, or crushed sandstone”

Revise the last paragraph of Article 1102.01 (a) (5) of the Standard Specifications to read:

“IL-4.75 and Stone Matrix Asphalt (SMA) mixtures which contain aggregate having absorptions greater than or equal to 2.0 percent, or which contain steal slag sand, shall have minimum surge bin storage plus haul time of 1.5 hours.”

Revise the first and second paragraphs of Articles 1030.06(c)(2) of the Standard Specifications to read:

“(2) Personnel. The Contractor shall provide a QC Manager who shall have overall responsibility and authority for quality control.  This individual shall maintain active certification as a Hot-Mix Asphalt Level II technician.

In addition to the QC Manager, the Contractor shall provide sufficient personnel to perform the required visual inspections, sampling, testing, and documentation in a timely manner.  Mix designs shall be developed by personnel with an active certification as a Hot-Mix Asphalt Level III technician.  Technicians performing mix design testing and plant sampling/testing shall maintain active certification as a Hot-Mix Asphalt Level I technician.  The Contractor may provide a technician trainee who has successfully completed the Department’s “Hot-Mix Asphalt Trainee Course” to assist in the activities completed by a Hot-Mix Asphalt Level I technician for a period of one year after the course completion date.  The Contractor may also provide a Gradation Technician who has successfully completed the Department's "Gradation Technician Course" to run gradation tests only under the supervision of a Hot-Mix Asphalt Level II Technician.  The Contractor shall provide a Hot-Mix Asphalt Density Tester who has successfully completed the Department's "Nuclear Density Testing” course to run all nuclear density tests on the job site.”

Add Article 1030.06(d)(3) to the Standard Specifications to read:

“(3) The Contractor shall take possession of any Department unused backup or dispute resolution HMA mixture samples or density specimens upon notification by the Engineer.  The Contractor shall collect the HMA mixture samples or density specimens from the location designated by the Engineer and may add these materials to RAP stockpiles according to Section 1031.”

Revise the second paragraph of Articles 1030.07(a)(11) and 1030.08(a)(9) of the Standard

Specifications to read:

“When establishing the target density, the HMA maximum theoretical specific gravity

(Gmm) will be based on the running average of four available Department test results

for that project. If less than four Gmm test results are available, an average of all

available Department test results for that project will be used. The initial Gmm will be

the last available Department test result from a QMP project. If there is no available

Department test result from a QMP project, the Department mix design verification test

result will be used as the initial Gmm.”

Revise the Quality Control Limits table in Article 1030.09(c) to read:

| CONTROL LIMITS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Parameter | IL-19.0, IL-9.5, IL-9.5FG, IL-19.0L, IL-9.5L |  | SMA-12.5, SMA-9.5 |  | IL-4.75 |  |
|  | Individual Test | Moving Avg. of 4 | Individual Test | Moving Avg. of 4 | Individual Test | Moving Avg. of 4 |
| % Passing: 1/ |  |  |  |  |  |  |
| 1/2 in. (12.5 mm) | ± 6 % | ± 4 % | ± 6 % | ± 4 % |  |  |
| 3/8 in. (9.5mm) |  |  | ± 4 % | ± 3 % |  |  |
| # 4 (4.75 mm) | ± 5 % | ± 4 % | ± 5 % | ± 4 % |  |  |
| # 8 (2.36 mm) | ± 5 % | ± 3 % | ± 4 % | ± 2 % |  |  |
| # 16 (1.18 mm) |  |  | ± 4 % | ± 2 % | ± 4 % | ± 3 % |
| # 30 (600 µm) | ± 4 % | ± 2.5 % | ± 4 % | ± 2.5 % |  |  |
| Total Dust Content # 200 (75 µm) | ± 1.5 % | ± 1.0 % |  |  | ± 1.5 % | ± 1.0 % |
| Asphalt Binder Content | ± 0.3 % | ± 0.2 % | ± 0.2 % | ± 0.1 % | ± 0.3 % | ± 0.2 % |
| Air Voids 2/ | ± 1.2 % | ± 1.0 % | ± 1.2 % | ± 1.0 % | ± 1.2 % | ± 1.0 % |
| Field VMA 3/ | -0.7 % | -0.5 % | -0.7 % | -0.5 % | -0.7 % | -0.5 % |

1/	Based on washed ignition oven or solvent extraction gradation.

2/	The air voids target shall be 3.2 to 4.8 percent.

3/	Allowable limit below minimum design VMA requirement.

Revise Article 1030.09(g)(2) of the Standard Specifications to read:

“(2)	The Contractor shall complete split verification sample tests listed in the Limits of Precision table in Article 1030.09(h)(1).”

In the Supplemental Specifications, replace the revision for the end of the third paragraph of

Article 1030.09(h)(2) with the following:

“When establishing the target density, the HMA maximum theoretical specific gravity

(Gmm) will be the Department mix design verification test result.”

Add after third sentence of Article 1030.09(b) to read:

“	If the Contractor and Engineer agree the nuclear density test method is not appropriate for the mixture, cores shall be taken at random locations determined according to the QC/QA document "Determination of Random Density Test Site Locations".  Core densities shall be determined using the Illinois Modified AASHTO T 166 or T 275 procedure.”

Revise Table 1 and Note 4/ of Table 1 in Article 406.07(a) of the Standard Specifications to read:

|  | Breakdown/Intermediate Roller (one of the following) | Final Roller (one or more of the following) | Density Requirement |
| --- | --- | --- | --- |
| IL-9.5, IL-9.5FG, IL-19.01/ | VD, P , TB, 3W, OT, OB | VS, TB, TF, OT | As specified in Section 1030 |
| IL-4.75 and SMA 3/ 4/ | TB, 3W, OT | TF, 3W | As specified in Section 1030 |
| Mixtures on Bridge Decks 2/ | TB | TF | As specified in Articles 582.05 and 582.06. |

“4/  The Contractor shall provide a minimum of two steel-wheeled tandem rollers (T B), and/or three-wheel (3W) rollers for breakdown, except one of the (TB) or (3W) rollers shall be 84 inches (2.14 m) wide and a weight of 315 pound per linear inch (PLI) (5.63 kg/mm) and one of the (TB) or (3W) rollers can be substituted for an oscillatory roller (OT). TF rollers shall be a minimum of 280 lb/in. (50 N/mm). The 3W and TB rollers shall be operated at a uniform speed not to exceed 3 mph (5 km/h), with the drive roll for TB rollers nearest the paver and maintain an effective rolling distance of not more than 150 ft (45 m) behind the paver.”

Add the following after the fourth paragraph of Article 406.13 (b):

“The plan quantities of SMA mixtures shall be adjusted using the actual approved binder and surface Mix Design’s Gmb.”

Revise first paragraph of Article 1030.10 of the Standard Specifications to read:

“A test strip of 300 ton (275 metric tons), except for SMA mixtures it will be 400 ton (363 metric ton), will be required for each mixture on each contract at the beginning of HMA production for each construction year according to the Manual of Test Procedures for Materials “Hot Mix Asphalt Test Strip Procedures”. At the request of the Producer, the Engineer may waive the test strip if previous construction during the current construction year has demonstrated the constructability of the mix using Department test results.”

Revise fourth paragraph of Article 1030.10 of the Standard Specifications to read:

“When a test strip is constructed, the Contractor shall collect and split the mixture according to the document “Hot-Mix Asphalt Test Strip Procedures”. The Engineer, or a representative, shall deliver split sample to the District Laboratory for verification testing. The Contractor shall complete mixture tests stated in Article 1030.09(a). Mixture sampled shall include enough material for the Department to conduct mixture tests detailed in Article 1030.09(a) and in the document “Hot-Mix Asphalt Mixture Design Verification Procedure“ Section 3.3. The mixture test results shall meet the requirements of Articles 1030.05(b) and 1030.05(d), except Hamburg wheel tests will only be conducted on High ESAL mixtures during production. To be considered acceptable to remain in place, the Department’s mixture test results shall meet the acceptable limits stated in Article 1030.09(i)(1).  In addition, no visible pavement distress such as, but not limited to, segregation, excessive coarse aggregate fracturing outside of growth curves, excessive dust balls, or flushing shall be present as determined by the Engineer.”