Regional Engineers

Jack A. Elston

Special Provision for Hot-Mix Asphalt

September 26, 2025

This special provision was developed by the Central Bureau of Materials to update the maximum theoretical specific gravity (Gmm) used in the calculation of HMA density and to allow HMA production to continue after a test strip has been constructed for all HMA Quality Management Programs (PFP, QCP, and QC/QA).  It has been revised to alleviate the potential for HMA binder courses left open over the winter and to address: HMA sample and specimen removal from District locations, quality control air voids target limits in the QC/QA quality management program, HMA test strip acceptance, and HMA performance testing.

This special provision should be inserted into all HMA paving contracts.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the January 16, 2026 and subsequent lettings.  The Project Coordination and Implementation Section will include a copy in the contract.

80456m

# Hot-Mix Asphalt (bde)

Effective:  January 1, 2024

Revised:  January 1, 2026

Add the following to the end of Article 406.06(c) of the Standard Specifications:

“	The amount of HMA binder course placed shall be limited to that which can be surfaced during the same construction season.”

Revise the fifteenth through eighteenth paragraphs of Article 406.14 of the Standard Specifications to read:

“	The mixture used in constructing acceptable HMA test strips will be paid for at the contract unit price. Unacceptable HMA test strips shall be removed and replaced at no additional cost to the Department.”

Revise the first and second paragraphs of Articles 1030.06(c)(2) of the Standard Specifications to read:

“	(2)	Personnel.  The Contractor shall provide a QC Manager who shall have overall responsibility and authority for quality control.  This individual shall maintain active certification as a Hot-Mix Asphalt Level II technician.

In addition to the QC Manager, the Contractor shall provide sufficient personnel to perform the required visual inspections, sampling, testing, and documentation in a timely manner.  Mix designs shall be developed by personnel with an active certification as a Hot-Mix Asphalt Level III technician.  Technicians performing mix design testing and plant sampling/testing shall maintain active certification as a Hot-Mix Asphalt Level I technician.  The Contractor may provide a technician trainee who has successfully completed the Department’s “Hot-Mix Asphalt Trainee Course” to assist in the activities completed by a Hot-Mix Asphalt Level I technician for a period of one year after the course completion date.  The Contractor may also provide a Gradation Technician who has successfully completed the Department's "Gradation Technician Course" to run gradation tests only under the supervision of a Hot-Mix Asphalt Level II Technician.  The Contractor shall provide a Hot-Mix Asphalt Density Tester who has successfully completed the Department's "Nuclear Density Testing” course to run all nuclear density tests on the job site.”

Add Article 1030.06(d)(3) to the Standard Specifications as follows:

“	(3)	The Contractor shall take possession of any Department HMA mixture samples or density specimens upon notification by the Engineer.  The Contractor shall collect the HMA mixture samples or density specimens from the location designated by the Engineer and may add these materials to RAP stockpiles according to Section 1031.”

Revise the second paragraph of Articles 1030.07(a)(11) and 1030.08(a)(9) of the Standard Specifications to read:

“	When establishing the target density, the HMA maximum theoretical specific gravity (Gmm) will be based on the running average of four available Department test results for that project.  If less than four Gmm test results are available, an average of all available Department test results for that project will be used.  The initial Gmm will be the last available Department test result from a QMP project.  If there is no available Department test result from a QMP project, the Department mix design verification test result will be used as the initial Gmm.”

Revise the Quality Control Limits table in Article 1030.09(c) to read:

| “CONTROL LIMITS |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Parameter | IL-19.0, IL-9.5, IL-9.5FG, IL-19.0L, IL-9.5L |  | SMA-12.5, SMA-9.5 |  | IL-4.75 |  |
|  | Individual Test | Moving Avg. of 4 | Individual Test | Moving Avg. of 4 | Individual Test | Moving Avg. of 4 |
| % Passing: 1/ |  |  |  |  |  |  |
| 1/2 in. (12.5 mm) | ± 6 % | ± 4 % | ± 6 % | ± 4 % |  |  |
| 3/8 in. (9.5mm) |  |  | ± 4 % | ± 3 % |  |  |
| # 4 (4.75 mm) | ± 5 % | ± 4 % | ± 5 % | ± 4 % |  |  |
| # 8 (2.36 mm) | ± 5 % | ± 3 % | ± 4 % | ± 2 % |  |  |
| # 16 (1.18 mm) |  |  | ± 4 % | ± 2 % | ± 4 % | ± 3 % |
| # 30 (600 µm) | ± 4 % | ± 2.5 % | ± 4 % | ± 2.5 % |  |  |
| Total Dust Content # 200 (75 µm) | ± 1.5 % | ± 1.0 % |  |  | ± 1.5 % | ± 1.0 % |
| Asphalt Binder Content | ± 0.3 % | ± 0.2 % | ± 0.2 % | ± 0.1 % | ± 0.3 % | ± 0.2 % |
| Air Voids 2/ | ± 1.2 % | ± 1.0 % | ± 1.2 % | ± 1.0 % | ± 1.2 % | ± 1.0 % |
| Field VMA 3/ | -0.7 % | -0.5 % | -0.7 % | -0.5 % | -0.7 % | -0.5 % |

1/	Based on washed ignition oven or solvent extraction gradation.

2/	The air voids target value shall be 3.2 to 4.8 percent.

3/	Allowable limit below minimum design VMA requirement.”

Revise Article 1030.09(g)(2) of the Standard Specifications to read:

“	(2)	The Contractor shall complete split verification sample tests listed in the Limits of Precision table in Article 1030.09(h)(1).”

In the Supplemental Specifications, replace the revision for the end of the third paragraph of Article 1030.09(h)(2) with the following:

“	When establishing the target density, the HMA maximum theoretical specific gravity (Gmm) will be the Department mix design verification test result.”

Replace the last sentence of the fourth paragraph of Article 1030.10 of the Standard Specifications with the following:

“	The mixture test results shall meet the requirements of Article 1030.05(d), except tensile strength and TSR testing will only be conducted on the first use of a mix design for the year and Hamburg wheel tests will only be conducted on High ESAL mixtures.  To be considered acceptable to remain in place, the Department’s mixture test results shall meet the acceptable limits stated in Article 1030.09(i)(1).  In addition, no visible pavement distress such as, but not limited to, segregation, excessive coarse aggregate fracturing outside of growth curves, excessive dust balls, or flushing shall be present as determined by the Engineer.”

Revise the tenth paragraph of Article 1030.10 of the Standard Specifications to read:

“	Production is not required to stop after a test strip has been constructed.”

Replace the eleventh paragraph of Article 1030.10 of the Standard Specifications with the following:

“	If an initial Hamburg wheel or I-FIT test fails to meet the requirements of Article 1030.05(d), the Department will verify the results by testing the retained gyratory cylinders.  Upon notification by the Engineer of a Hamburg wheel or I-FIT test failure on the retained gyratory cylinders, the Contractor shall substitute an approved mix design, submit a new mix design for mix verification testing according to Article 1030.05(d), or pave 250 tons with or without an adjustment and resample for Department Hamburg wheel and I-FIT testing as directed by the Engineer.  Paving may continue as long as all other mixture criteria is being met.  If Hamburg wheel or I-FIT tests on the resampled HMA fail, production of the affected mixture shall cease and the Contractor shall substitute an approved mix design or submit a new mix design for mix verification testing according to Article 1030.05(d).”

80456