Regional Engineers

Jack A. Elston

Special Provision for Inlet Filters

January 9, 2026

This special provision was developed by the Central Bureau of Materials to increase the options available for inlet filters and to update ASTM testing standards.

This special provision should be inserted into contracts with INLET FILTERS.

The districts should include the BDE Check Sheet marked with the applicable special provisions for the April 24, 2026 and subsequent lettings.  The Project Coordination and Implementation Section will include a copy in the contract.

80483m

# Inlet filters

Effective:  April 1, 2026

Revise the first paragraph of Article 1081.15(h) of the Standard Specifications to read:

“	(h)	Inlet Filters.  An inlet filter shall consist of a steel frame with a two piece geotextile fabric bag or a single reinforced geotextile fabric bag attached with a stainless steel band and locking cap that is suspended from the frame.  A clean, used bag and a used steel frame in good condition meeting the approval of the Engineer may be substituted for new materials.  Materials for the inlet filter assembly shall be according to the following.”

Revise Article 1081.15(h)(3) of the Standard Specifications to read:

“	(3)	Geotextile Fabric Bag.  The sediment bag shall have a minimum silt and debris capacity of 2.0 cu ft (0.06 cu m).  The sediment bag shall also meet one of the following options.

  - OPTION 1.  Two piece geotextile fabric bag.

The inner filter bag shall be constructed of a polypropylene geotextile fabric according to the following.

| Inner Filter Bag |  |  |
| --- | --- | --- |
| Material Property | Test Method | Minimum Average Roll Value |
| Grab Tensile Strength | ASTM D 4632 | 100 lb (45 kg) |
| Grab Tensile Elongation | ASTM D 4632 | 50% |
| Puncture Strength | ASTM D 4833/ ASTM D 6241 | 65 lb (29 kg) |
| Trapezoidal Tear | ASTM D 4533 | 45 lb (20 kg) |
| UV Resistance | ASTM D 4355 | 70% at 500 hours |
| Apparent Opening Size | ASTM D 4751 | No. 70 (212 μm) sieve |
| Permittivity | ASTM D 4491 | 2.0/sec |
| Water Flow Rate | ASTM D 4491 | 145 gpm/sq ft (5900 Lpm/sq m) |

The outer reinforcement bag shall be constructed of a polyester mesh material according to the following.

| Outer Reinforcement Bag |  |  |
| --- | --- | --- |
| Material Property | Test Method | Value |
| Content | ASTM D 629 | Polyester |
| Weight | ASTM D 3776 | 4.55 oz/sq yd (155 g/sq m) ± 15% |
| Apparent Opening Size | ASTM D 4751 | No. 30 (600 μm) sieve |
| Water Flow Rate | ASTM D 4491 | 225 gpm/sq ft (9150 Lpm/sq m) |
| Burst | ASTM D 3786/ ASTM D 3787 | 120 psi (830 kPa) min. |
| Thickness | ASTM D 1777 | 0.040 ± 0.0050 in. (1.0 ± 0.1 mm) |

b.	OPTION 2.  Reinforced geotextile fabric bag.

The filter bag shall be constructed of a polypropylene geotextile fabric reinforced with continuous filament fiberglass according to the following.

| Reinforced Filter Bag |  |  |
| --- | --- | --- |
| Material Property | Test Method | Value or Minimum Average Roll Value |
| Weight | ASTM D 3776 | 5.00 oz/sq yd (170 g/sq m) ± 15% |
| Grab Tensile Strength | ASTM D 4632 | 200 lb (90 kg) |
| Grab Tensile Elongation | ASTM D 4632 | 50% |
| Puncture Strength | ASTM D 4833/ ASTM D 6241 | 95 lb (42 kg) |
| Trapezoidal Tear | ASTM D 4533 | 70 lb (31 kg) |
| Burst Strength | ASTM D 3786/ ASTM D 3787 | 325 psi (2240 kPa) |
| UV Resistance | ASTM D 4355 | 70% at 500 hours |
| Apparent Opening Size | ASTM D 4751 | No. 70 (212 μm) sieve |
| Permittivity | ASTM D 4491 | 2.0/sec |
| Water Flow Rate | ASTM D 4491 | 145 gpm/sq ft (5900 Lpm/sq m) |

- Certification.  The manufacturer shall furnish a certification with each shipment of inlet filters, stating the amount of product furnished and that the material complies with these requirements.”

80483