# friction aggregate (D1)

Effective:  January 1, 2011

Revised:  December 1, 2021

# Revise Article 1004.03(a) of the Standard Specifications to read:

“1004.03	Coarse Aggregate for Hot-Mix Asphalt (HMA).  The aggregate shall be according to Article 1004.01 and the following.

(a)	Description.  The coarse aggregate for HMA shall be according to the following table.

| Use | Mixture | Aggregates Allowed |  |  |
| --- | --- | --- | --- | --- |
| Class A | Seal or Cover | Allowed Alone or in Combination 5/: Gravel Crushed Gravel Carbonate Crushed Stone Crystalline Crushed Stone Crushed Sandstone Crushed Slag (ACBF) Crushed Steel Slag Crushed Concrete |  |  |
| HMA Low ESAL | Stabilized Subbase or Shoulders | Allowed Alone or in Combination 5/: Gravel Crushed Gravel Carbonate Crushed Stone Crystalline Crushed Stone Crushed Sandstone Crushed Slag (ACBF) Crushed Steel Slag1/ Crushed Concrete |  |  |
| HMA High ESAL Low ESAL | Binder IL-19.0 or IL-19.0L SMA Binder | Allowed Alone or in Combination 5/ 6/: Crushed Gravel Carbonate Crushed Stone2/ Crystalline Crushed Stone Crushed Sandstone Crushed Slag (ACBF) Crushed Concrete3/ |  |  |
| HMA High ESAL Low ESAL | C Surface and Binder IL-9.5 IL-9.5FG or IL-9.5L | Allowed Alone or in Combination 5/: Crushed Gravel Carbonate Crushed Stone2/ Crystalline Crushed Stone Crushed Sandstone Crushed Slag (ACBF) Crushed Steel Slag4/ Crushed Concrete3/ |  |  |
| HMA High ESAL | D Surface and Binder IL-9.5 or IL-9.5FG | Allowed Alone or in Combination 5/: Crushed Gravel Carbonate Crushed Stone (other than Limestone)2/ Crystalline Crushed Stone Crushed Sandstone Crushed Slag (ACBF) Crushed Steel Slag4/ |  |  |
|  |  | Other Combinations Allowed: |  |  |
|  |  | Up to... |  | With... |
|  |  | 25% Limestone |  | Dolomite |
|  |  | 50% Limestone |  | Any Mixture D aggregate other than Dolomite |
|  |  | 75% Limestone |  | Crushed Slag (ACBF) or Crushed Sandstone |
| HMA High ESAL | E Surface IL-9.5 SMA Ndesign 80 Surface | Allowed Alone or in Combination 5/ 6/: Crushed Gravel Crystalline Crushed Stone Crushed Sandstone Crushed Slag (ACBF) Crushed Steel Slag No Limestone. |  |  |
|  |  | Other Combinations Allowed: |  |  |
|  |  | Up to... | With... |  |
|  |  | 50% Dolomite2/ | Any Mixture E aggregate |  |
|  |  | 75% Dolomite2/ | Crushed Sandstone, Crushed Slag (ACBF), Crushed Steel Slag, or Crystalline Crushed Stone |  |
|  |  | 75% Crushed Gravel2/ | Crushed Sandstone, Crystalline Crushed Stone, Crushed Slag (ACBF), or Crushed Steel Slag |  |
| HMA High ESAL | F Surface IL-9.5 SMA Ndesign 80 Surface | Allowed Alone or in Combination 5/ 6/: Crystalline Crushed Stone Crushed Sandstone Crushed Slag (ACBF) Crushed Steel Slag No Limestone. |  |  |
|  |  | Other Combinations Allowed: |  |  |
|  |  | Up to... | With... |  |
|  |  | 50% Crushed Gravel2/ or Dolomite2/ | Crushed Sandstone, Crushed Slag (ACBF), Crushed Steel Slag, or Crystalline Crushed Stone |  |

- Crushed steel slag allowed in shoulder surface only.

- Carbonate crushed stone (limestone) and/or crushed gravel shall not be used in SMA Ndesign 80.

- Crushed concrete will not be permitted in SMA mixes.

- Crushed steel slag shall not be used as binder.

- When combinations of aggregates are used, the blend percent measurements shall be by volume.”

- Combining different types of aggregate will not be permitted in SMA Ndesign 80.”