# ROCKFILL

Effective: January 1, 2010

Revised: April 1, 2022

Description.  This work shall consist of the furnishing and placement of rockfill where unstable and/or unsuitable materials have been removed below the plan bedding grade of proposed cast-in-place and/or precast concrete box culverts.  This work shall be done as shown on the plans and as directed by the Engineer.

Materials.  Materials shall meet the following requirements of the Standard Specifications:

Item	Section

CA 07 and CA 11	  1004

Rockfill	  1005

The gradation of rockfill shall be selected based on the following table:

Material:  Crushed Stone, Crushed Gravel, and Crushed Concrete

| Sieve Size | Option 1 Percent Passing | Option 2 Percent Passing |
| --- | --- | --- |
| 3 inches (75 mm) | 100 |  |
| 2 1/2 inches (63 mm) | 95 ± 5 | 100 |
| 2 inches (50 mm) | 60 ± 15 | 93 ± 7 |
| 1 1/2 inches (37.5 mm) | 15 ± 15 | 55 ± 20 |
| 1 inch (25 mm) | 3 ± 3 | 8 ± 8 |
| 1/2 inch (12.5 mm) |  | 3 ± 3 |

Geotechnical fabric for ground stabilization shall be nonwoven and meeting the requirements of Article 1080.02 of the Standard Specifications may be necessary dependent upon subgrade soil conditions.  The Engineer shall make the determination if Geotechnical fabric utilization is necessary.

Construction Requirements.  Unstable and/or unsuitable soil shall be excavated according to Article 502.11 of the Standard Specifications.  Rockfill shall be placed following the excavation of the unstable and/or unsuitable material. The maximum nominal thickness when compacted shall be 24 in. (600 mm).  Each lift of aggregate shall be compacted to the satisfaction of the Engineer.

The rockfill shall be capped with material meeting the aggregate gradations of CA 07 or CA 11 according to Article 1004.01.  The minimum cap thickness shall be 3 in. (75 mm).

The fabric, if required, shall be installed according to the applicable portions of Section 210 of the Standard Specifications.

Method of Measurement.  Rockfill will be measured for payment in cubic yards (cubic meters).

Geotechnical fabric for ground stabilization will be measured for payment according to Article 210.05 of the Standard Specifications.

Basis of Payment.  Rockfill will be paid for at the contract unit price per cubic yard (cubic meter) for ROCKFILL.

Geotechnical fabric for ground stabilization will be paid for according to Article 210.06 of the Standard Specifications.  When the contract does not contain a pay item for the fabric and this item is required, it will be paid for according to Article 109.04 of the Standard Specifications.

Box culverts, removal and disposal of unstable and unsuitable materials, porous granular bedding material, and the excavation required for bedding will be paid for according to Section 540 of the Standard Specifications.