## EMBANKMENT II (D1)

Effective: March 1, 2011

Revised: November 1, 2013

Description.  This work shall be according to Section 205 of the Standard Specifications except for the following.

Material.  Reclaimed asphalt shall not be used within the ground water table or as a fill if ground water is present. The RAP used shall be according to the current Bureau of Materials and Physical Research Policy Memorandum, “Reclaimed Asphalt Pavement (RAP) for Aggregate Applications”. Gradation deleterious count shall not exceed 10% of total RAP and 5% of other by total weight.

CONSTRUCTION REQUIREMENTS

Samples.  Embankment material shall be sampled and tested before use.  The contractor shall identify embankment sources, and provide equipment as the Engineer requires, for the collection of samples from those sources.  Samples will be furnished to the Geotechnical Engineer a minimum of three weeks prior to use in order that laboratory tests for compaction can be performed.  Embankment material placement cannot begin until tests are completed.

Placing Material.  In addition to Article 202.03, broken concrete, reclaimed asphalt with no expansive aggregate, or uncontaminated dirt and sand generated from construction or demolition activities shall be placed in 6 inches (150 mm) lifts and disked with the underlying lift until a uniform homogenous material is formed.  This process also applies to the overlaying lifts.  The disk must have a minimum blade diameter of 24 inches (600 mm).

When embankments are to be constructed on hillsides or existing slopes that are steeper than 3H:1V, steps shall be keyed into the existing slope by stepping and benching as shown in the plans or as directed by the Engineer.

Compaction.  Soils classification for moisture content control will be determined by the Soils Inspector using visual field examination techniques and the IDH Textural Classification Chart.

When tested for density in place each lift shall have a maximum moisture content as follows.

a)	A maximum of 110 percent of the optimum moisture for all forms of clay soils.

b)	A maximum of 105 percent of the optimum moisture for all forms of clay loam soils.

Stability.  The requirement for embankment stability in article 205.04 will be measured with a Dynamic Cone Penetrometer (DCP) according to the test method in the IDOT Geotechnical Manual.  The penetration rate must be equal or less than 1.5 inches (38 mm) per blow.

Basis of Payment.  This work will not be paid separately but will be considered as included in the various items of excavation.