This special provision was originally developed by the Bureau of Materials & Physical Research at the recommendation of the Illinois Highway Development Council to allow temporary rubber ramps to be used as an option around frames and grates during milling and resurfacing operations.

It should be inserted into contracts involving milling and resurfacing on contracts with permanent posted speed limits up to 40 mph.

revised reference to "Class SI" concrete with "Class PP" and replaced 72 hours w/ reference to Art 701.17(e)(3)b;

It should be included for the April 29, 2011 and subsequent lettings.

# drainage and inlet protection under traffic (d1)

Effective:  April 1, 2011

Revised:  April 2, 2011

Add the following to Article 603.02 of the Standard Specifications:

“	(i)	Temporary Hot-Mix Asphalt (HMA) Ramp (Note 1) ……………………………….	1030

(j)	Temporary Rubber Ramps (Note 2)

Note 1. The HMA shall have maximum aggregate size of 3/8 in. (95 mm).

Note 2. The rubber material shall be according to the following.

| Property | Test Method | Requirement |
| --- | --- | --- |
| Durometer Hardness, Shore A | ASTM D 2240 | 75 15 |
| Tensile Strength, psi (kPa) | ASTM D 412 | 300 (2000) min |
| Elongation, percent | ASTM D 412 | 90 min |
| Specific Gravity | ASTM D 792 | 1.0 - 1.3 |
| Brittleness, F (C) | ASTM D 746 | -40 (-40)” |

Revise Article 603.07 of the Standard Specifications to read:

“603.07	Protection Under Traffic.  After the casting has been adjusted and the Class PP concrete has been placed, the work shall be protected by a barricade and two lights according to Article 701.17(e)(3)b.

When castings are under traffic before the final surfacing operation has been started, properly sized temporary ramps shall be placed around the drainage and/or utility castings according to the following methods.

(a)	Temporary Asphalt Ramps.  Temporary hot-mix asphalt ramps shall be placed around the casting, flush with its surface and decreasing to a featheredge in a distance of 2 ft (600 mm) around the entire surface of the casting.

(b)	Temporary Rubber Ramps.  Temporary rubber ramps shall only be used on roadways with permanent posted speeds of 40 mph or less and when the height of the casting to be protected meets the proper sizing requirements for the rubber ramps as shown below.

| Dimension | Requirement |
| --- | --- |
| Inside Opening | Outside dimensions of casting + 1 in. (25 mm) |
| Thickness at inside edge | Height of casting 1/4 in. (6 mm) |
| Thickness at outside edge | 1/4 in. (6 mm) max. |
| Width, measured from inside opening to outside edge | 8 1/2 in. (215 mm) min |

Placement shall be according to the manufacturer’s specifications.

Temporary ramps for castings shall remain in place until surfacing operations are undertaken within the immediate area of the structure.  Prior to placing the surface course, the temporary ramp shall be removed.  Excess material shall be disposed of according to Article 202.03.”