# TRAFFIC SIGNAL POST

Effective: May 22, 2002

Revised: March 1, 2025

875.01TS

Revise Article 1077.01 (c) of the Standard Specifications to read:

(c)	Anchor Rods.  The anchor rods shall be a minimum of 5/8 in. in diameter and 16 in. 	long and shall be according to Article 1006.09. The anchor rods shall be threaded 	approximately 6 in. at one end and have a bend at the other end. The first 12 in. at the 	threaded end shall be galvanized. One each galvanized nut and trapezoidal washer shall 	be furnished with each anchor rod. The washer shall be properly sized to fully engage 	and sit flush on all sides of the slot of the base plate.

Revise the first sentence of Article 1077.01 (d) of the Standard Specifications to read:

All steel posts and bases shall be hot dipped galvanized steel according to AASHTO M 111.  If the Department approves painting, powder coating by the manufacturer will be required over the galvanization in accordance with 851.01TS TRAFFIC SIGNAL PAINTING Special Provisions.